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POLY-TERT- AMYLPHENOLDISULFIDE

EINECS : Conforms

	SPECIFICATIONS
	VALUES
	METHODS

	Sulfur content (% weight)

Water content

Particle size (dry sieving)

        passing 840 SYMBOL 109 \f "Symbol"m sieve

        passing 300 SYMBOL 109 \f "Symbol"m sieve


	SYMBOL 179 \f "Symbol" 20 % / SYMBOL 163 \f "Symbol" 22 %

SYMBOL 163 \f "Symbol" 2 %

SYMBOL 179 \f "Symbol" 99 %

SYMBOL 179 \f "Symbol" 98 %


	SOP QC - 113 e (Combustion, IR)

SOP QC - 114 e (IR)

SOP QC - 114 e


The above commercial specifications are guaranteed ; they were established using the test methods which were in force at the plant at the time of despatch of the product, and are in accordance with any applicable revision references.

PACKAGING

- Box (31 x 36 x 66) with PE inner bag of 15 kg net (16.5 kg gross).

- Pallet of 18 bags ( 110 x 96 x 145), 270 kg net (290 kg gross).

- Pallet of 27 bags ( 110 x 96 x 211), 405 kg net (469 kg gross).

SAFETY / PRECAUTIONS DURING USE

Please refer to the safety data sheet before handling.

HANDLING / STORAGE

Please refer to the safety data sheet.

VULTACSYMBOL 226 \f "Symbol"5

TECHNICAL DATA

VULTACSYMBOL 226 \f "Symbol"5 is a beige, free flowing powder. It is nearly odourless. It contains 25% powdering aid.

VULTACSYMBOL 226 \f "Symbol"5 is nitrosamine free.

CHEMICAL NATURE OF THE PREPARATION

VULTACSYMBOL 226 \f "Symbol"3 : 75 %

Silica gel : 25 %

USES

Vulcanizing agent.

PHYSICAL DATA

Density (25°C)
1435 kg/m3
Softening temperature
(approx.) 71 °C

Solubility
In water : insoluble
The information contained in this document is based on trials carried out by our Research Centres and data selected from the literature, but      shall in no event be held to constitute or imply any warranty, undertaking, express or implied commitment from our part. Our formal specifications define the limit of our commitment. No liability whatsover can be accepted by Elf Atochem with regard to the handling, processing or use of the product or products concerned which must in all cases be employed in accordance with all relevant laws and/or regulations in force in the country or countries concerned.

please check with MLPC International that this data sheet is the latest available version.

YOUR CONTACT : PATRICIA FOURTEAU – ( : 33 5 58 57 02 24 - FAX : 33 5 58 57 02 02

[image: image2.png]RS




209, Avenue Charles Despiau - 40370 RION-DES-LANDES (France) - ( : (33) 05 58 57 02 00 - Fax : (33) 05 58 57 02 02

Ref. : DTF-Thio/C.1
CDS N° : A-02040

Updated : 07.04.99
  Revision : 7
_920379428

_976609442

